## Slide 1
METALMAN TRIALS DETAILS
Saptagiri Eng.Pvt.Ltd

## Slide 2
03
02
01
04
05
07
06
09
08
11
10
13
12
14
15
16
A
B
D
C
At top Side E & F
F
E
JIG MAPPING
Saptagiri Eng.Pvt.Ltd

## Slide 3
GUN PARAMETER
Gun Parameter | 
KV | 70
CURRENT | 80
TOTAL AIR PRESSURE | 6.0 m3/4r
FLUEDIZE AIR | 0.1 Bar
POWDER OUT PUT | 47 gm/min
Saptagiri Eng.Pvt.Ltd
TRIALS ON 8 & 9 th Mar 2024
Jig Mapping DFT report

## Slide 4
Supplier : Metalman Auto pvt. Ltd.` |  |  |  |  |  |  | 
Part Name: DUST COVER J1A Part Number: S2DF02703O |  |  |  |  | Date : 21.02.2024 |  | 
Observation |  |  |  |  |  |  | 
Sn. | A | B | C | D | E | F | Average
Min | 82 | 80 | 76 | 76 | 93 | 93 | 83
Max | 171 | 213 | 150 | 151 | 195 | 182 | 177
Total process qty |  |  | 96 |  |  |  | 
Total rejection for less DFT |  |  | 10 |  |  |  | 
Rejection % |  |  | 10.4% |  |  |  | 
Supplier : Metalman Auto pvt. Ltd. |  |  |  |  |  |  | 
Part Name: DUST COVER J1A Part Number: S2DF02703O |  |  |  |  | Date : 08 & 9..03.2024 |  | 
Observation |  |  |  |  |  |  | 
Sn. | A | B | C | D | E | F | Average
Min | 74 | 82 | 94 | 76 | 102 | 105 | 89
Max | 167 | 156 | 144 | 178 | 176 | 145 | 161
Total process qty |  |  | 96 |  |  |  | 
Total rejection for less DFT |  |  | 3 |  |  |  | 
Rejection % |  |  | 3.1% |  |  |  | 
Suplier : Metalman Auto pvt. Ltd. |  |  |  |  |  |  | 
Part Name: DUST COVER J1A Part Number: S2DF02703O |  |  |  |  | Date : 06.02.2024 |  | 
Observation |  |  |  |  |  |  | 
Sn. | A | B | C | D | E | F | Average
Min | 68 | 82 | 69 | 81 | 82 | 69 | 75
Max | 115 | 126 | 134 | 145 | 123 | 115 | 126
Total process qty |  |  | 80 |  |  |  | 
Total rejection for less DFT |  |  | 20 |  |  |  | 
Rejection % |  |  | 25.0% |  |  |  | 
Trial first
Trial Second
Trial Third
TRIALS DETAILS FOR DFT
Saptagiri Eng.Pvt.Ltd

## Slide 5
Chart: 
| Trial First | Trial Second | Trial Third
Visual Defect rej % | 7.8 | 19.8 | 4.2
DFT rej % | 25 | 10.4 | 3.2
POWDER COATING REJECTION % FOR DFT & VISUAL DEFECTS
Saptagiri Eng.Pvt.Ltd

## Slide 6
Trials for 4 th , 5 ,6 & 7 th
Saptagiri Eng.Pvt.Ltd

## Slide 7
Saptagiri Eng.Pvt.Ltd
TRIALS & MATERIAL SUPPLIES DETAILS |  |  |  |  | 
PART NAME | : DUST COVER J1A |  | PART NO | : S2DF02703O | 
Trial Details: |  |  |  |  | 
Sn of Trails | Trial Date | Trial qty in nos | Inhouse rej % for Visual Defects | Inhouse rej % for less DFT | Total
I st | 13-Mar-24 | 540 | 3.5% | 5.9% | 9.4%
II nd | 14-Mar-24 | 540 | 3.9% | 6.3% | 10.2%
III rd | 16-Mar-24 | 540 | 4.4% | 7.0% | 11.4%
IV th | 18-Mar-24 | 540 | 3.7% | 5.2% | 8.9%
Material Supplies details: |  |  |  |  | 
Material Supplies Date | Invoice date | Invoice No | Invoice qty in nos | Supplied to ETL plant | ETL remark
14-Mar-24 | 14-Mar-24 | 16305 | 500 | E92 | No complaint
16-Mar-24 | 16-Mar-24 | 16400 | 500 | E92 | No complaint
18-Mar-24 | 18-Mar-24 | 16470 | 500 | E92 | No complaint
20-Mar-24 | 20-Mar-24 | 16601 | 500 | E92 | No complaint

## Slide 8
Chart: 
| Trial First | Trial Second | Trial Third | Trial fourth | Trial fifth | Trial sixth | Trial Seventh
Visual Defect rej % | 7.8 | 19.8 | 4.2 | 3.5 | 3.9 | 4.4 | 3.7
DFT rej % | 25 | 10.4 | 3.2 | 5.9 | 6.3 | 7 | 5.2
POWDER COATING REJECTION % FOR DFT & VISUAL DEFECTS
Saptagiri Eng.Pvt.Ltd

## Slide 9
Conclusion:
Saptagiri Eng.Pvt.Ltd
Rejection % for Visual defects :3.5 – 4.4 %
Rejection % for less DFT :5.2 – 7.0 %

## Slide 10
Thank You
Saptagiri Eng.Pvt.Ltd