## Slide 1: XF1F1 LOW HARDNESS Action Plan

## Slide 2
NG Part | OK Part
CONDITIONS FOR OCCURRENCE
● Phenomenon: LOW HARDNESS
Trouble content
・Supplier: Endurance Technologies Ltd.
・Model: XF1F1
・Parts name: Front Fork
・Part No.:
・Date of Occurrence:06.09.2024
・Qty NG: 40 Nos
●Parts Stock check results
Action
Area | Total Stock | Checked | Checking Method | NG Qty | Status
Dekson Casting Ltd | 50 | 50 | By Hardness Tester | 0 | All available stock qty. verified & found NG
ETL | 40 | 40 | By Hardness Tester | 240 | 

## Slide 3
UNDERSTANDING OF ACTUAL CONDITION AND CONTROL
Process Flow
Possible defect occurrence area.
R M Inward
Melting
Gravity Die Casting
Riser Cutting
Final Inspection
SPM Drilling
1
Belt Grinding
Packing and Dispatch
Heat Treatment
Grinding and Fettling

## Slide 4
UNDERSTANDING OF ACTUAL CONDITION
● Understanding the actual cause – (Factor analysis)
Man
Method
Material
Machine
Less Awareness
Training not followed for New inspector and operator
Unskilled operator & Inspector
Metal Temp high/low
Hardness less than specification
Quenching tank not clean
Heat Treatment Furnance Fan bearing jam
temp variation

## Slide 5
FACTS VERIFICATION
SR NO | 4M | PROBABLE CAUSES | FACTS VERIFICATION | Judgment
1 | MAN | Less Awareness | verify Awareness of operator and found Not Ok | O
 |  | Unskilled operator & Inspector | Verified skill level of Inspector & fond Ok as per the skill matrix | O
 |  | Training not followed for New inspector and operator | Verified training record and work procedure for inadequacy while appointing new inspector and found Ok. | O
2 | MACHINE | Fan bearing not ok Quenching tank not clean | Heat Treatment Furnance Fan bearing jam & Also Monthly cleaning tank frequency. | x
3 | METHOD | temp High/low | temp check found ok | O
 |  | Die temp variation | Die temp check found ok | O

## Slide 6
ROOT CAUSE ESTABLISHMENT (WHY-WHY ANALYSIS)
 | WHY – 1 | WHY- 2 | WHY -3 | WHY-4 | Why-5
Occurrence | Hardness less than specification | Heat Treatment Furnance Fan suddenly Off &Quenching tank not clean, | Furnance Fan bearing jam | air circulation not proper | 
Outflow | Hardness less than specification | Not detected in Inspection | Inspection done on sampling basis | - | -
● Root cause establishment (Why-Why Analysis)

## Slide 7
COUNTERMEASURES
 | Cause | Countermeasure | Tgt. Dt. | Status
Supplier End | <Occurrence > | 1.Fan Bearing changed & its Life monitoring started. 2. Fan check point added in heat Treatment WI. 3. Water tank cleaning frequency changed to weakly. 4. Tank cleaning check point added in heat Treatment WI. | 15.09.2024 | Completed
Supplier End | <Outflow> | Checking Hardness in every Lot after Heat Treatment. | 15.09.2024 | Completed
ETL End | <Outflow> | Start inspection in every lot. | 15.09.2024 | Completed

## Slide 8
GDC
Low Hardness 85 BHN | Hardness OK 105 BHN
Shop: GDC
Operation: Pouring
AFTER
Implementation Date: 15.09.2024
BEFORE