## Slide 1: MAP ALLOYS
Analysis report and Action plan for Leakage issue in Integral Caliper Body-raw.

## Slide 2
Corrective Action / 8D Report
On
Leakage observed in Integral Caliper body Raw.
Date: -24.10.2024.
Problem Analysis and Corrective Action Report

## Slide 3
D1 : CFT for Problem Solving
Problem Definition : |  | Leakage observed in caliper body raw | Defect Photo
Part No./Name | : | Calliper Body Raw | 
Customer/Location | : | ETL/ Auramgabad | 
Advik Plant Name / No. | : | K-226/2 ,Waluj MIDC, Sambhajinagar | 
Complaint Date / Time | : | 24.10.2024 | 
Rejection Qty | : | 1 no. | 
Repeated / New | : | repeated | 
Reported By | : | Mr. Raviraj Gaikward | 
Attended By | : | Mr.Navnath G | 
Closing Date (Target) | : | In-Process. | 
D2 : Complaint Details:
Sr. No. | Name | Department | Designation
1 | Mr. S.K Dash | Operation | Operation Head
2 | Mr. Manish Kolte | Quality | Quality Head
3 | Mr.Rajesh Pandey | Quality | Assist. Manager
4 | Mr. Moreshwar Patil | Quality | Quality Engineer
5 | Mr. Bhaskar Madape | Production | Production Incharge
6 | Mr.Anil Dhange | Die Maint. | Die Maint. Incharge
Leakage

## Slide 4
D3 : Interim / Containment Action
Sr. No. | Containment Area / Location | Date | Available Qty. | Segregation Qty | OK Qty. | NG Qty. | Dispatch / Remarks
1 | Customer End |  |  |  |  |  | 
2 | Warehouse |  |  |  |  |  | 
3 | Plant Dispatch Area |  |  |  |  |  | 
4 | Final Inspection & Assembly Line |  |  |  |  |  | 
5 | Machine Shop |  |  |  |  |  | 
6 | Incoming Insp. |  |  |  |  |  | 
7 | Receipt Store |  |  |  |  |  | 
8 | Supplier End At Final inspection. |  |  |  |  |  | 
9 | At Production stage (Please Specify) |  |  |  |  |  | 
10 | Other Location (Please Specify) |  |  |  |  |  | 
Interim / Containment Actions Closure - Date: Time: Shift:

## Slide 5
Process Flow Information
  Receipt of raw material
Incoming inspection of
AC2A Alloy
Incoming raw material inspection(Sand)
Storage of raw material.
Fettling/Grinding
Runner/Riser Cutting
Decoring
Casting
Note: Fill Red Color in process Block where defect is occurred.
Degassing (if DI not ok)
Holding molten metal in holding chamber
Melt treatment inside chamber and at holding chamber
Continuous charging and melting
DI and Spectro Check
N2 Lance Degassing
Die preparation & Die loading
Sand core
Heat Treatment
Heat Number punching & shot blasting.
Transfer to Inspection & Final inspection
Packing

## Slide 6
D4 : Root Cause Analysis: Ishikawa Diagram
Leakage issue in Integral Caliper body Raw.
Man
Machine
Method
Material
Measurement
Environment
Unskilled Operator
Machine Jerk and Vibration
Chemical composition not ok
Spectro not Calibrated.
Low illumination level (Rec: 600 min lux)
Pouring delay
Short pouring
Less metal temp.
Less die coat application
Machine parameters are not ok
Excess metal filling time.
New Operator
Wrong Grade material use.
Inspection frequency not defined.
Less venting
No smooth Feeding of metal in cavity.

## Slide 7
D4 : Validation of Probable Causes:
Sr. No. | Area/Condition | Probable Cause | Validation | Observation (Significant/ Non-Significant)
1 | Man | Unskilled Operator | Operator is skilled . | Non-Significant
 | Man | New Operator | Operator working from last 1.6 years | Non-Significant
2 | Machine | Machine jerk and vibration | No jerk and vibration in machine | Non-Significant
 |  | Machine parameters are not ok | Machine parameters like solidification | Non-Significant
 |  | Less Venting | Less gas pass from the cavity. | Non-Significant
3 | Method | Pouring delay by operator | No Pouring delay by Operator | Non-Significant
 |  | Short poring | No short pouring | Non-Significant
 |  | Less metal temp | Metal temperature found 718C | Non-Significant
 |  | Less die coat application | Die coat application found Ok | Non-Significant
 |  | Excess metal filling time | No excess metal filling time . | Non - Significant
 |  | No smooth Feeding of metal in cavity at leak area. | No smooth flow of metal due to pouring cup depth excess . | Significant
4 | Material | Chemical composition not ok. | Chemical composition found Ok | Non-Significant
5 | Measurement | Spectro machine not calibrated | Spectro machine calibrated. | Non-Significant
6 | Environment | Low illumination level (Rec: 600 min lux) | Lux level checked found - 760 | Non-Significant

## Slide 8
D4 : Why-Why Analysis for Occurrence:
Cause(s)  | Cause1 | Cause 2 (As Applicable)
Why- Why | Leakage after machining | 
Why 1 | Metal turbulence in cavity at leak area | 
Why 2 | No smooth flow of molten metal in cavity. | 
Why 3 | Pouring cup depth excess than required. | 
Why 4 |  | 
Why 5 |  | 
Final Root Cause | Pouring cup depth excess than required. | 

## Slide 9
D4 : Why-Why Analysis for Outflow :
Cause(s)  | Cause1 | Cause 2 (As Applicable)
Why- Why | N/A | 
Why 1 |  | 
Why 2 |  | 
Why 3 |  | 
Why 4 |  | 
Why 5 |  | 
Final Root Cause |  | 

## Slide 10
D5 : Corrective Actions (Occurrence & Outflow)
Sr. No. | Action to be taken | Resp. | Target Date | Status | Remarks
1. | Pouring cup depth decrease and slop provided for smooth flow of metal in cavity. | Mr. Anil Dhande / P.N.Patil. | 25.10.2024 | Completed. | Lot is to be produce.
Sr. No. | Action to be taken | Resp. | Target Date | Status | Remarks
1. | Quality Alert displayed. Training has been provided to the inspector. | Mr. Navnath G | 11.09.2024 | Completed | Ok
2. Outflow:
1. Occurrence :

## Slide 11
D6 : Verification of Corrective Actions
Sr. No. | Action taken | Verified By | Verification Date | Status | Remarks
1. | Pouring cup depth decrease and slop provided for smooth flow of metal in cavity. | Rajesh Pandey | 25.10.2024. | Completed | 
Note: Please attach evidences here. Insert evidences as objects.
Pouring cup depth decreases from 45mm to 32 mm for smooth pouring.
After Correction
Before Correction
Before correction pouring cup depth was 45 mm
Before correction pouring cup depth was 32 mm

## Slide 12
D7(A) : Preventive Actions
Sr. No. | Action taken | Resp. | Target Date | Status | Remarks
1. | we will update in design of pouring cup. | Mr. Rajesh Pandey | 15.11.2024 | Completed. | 
Horizontal Deployment : |  |  |  |  | 
Sr. No. | Product Scope | Resp. | Impletn. Date | Status | Remark

## Slide 13
D7(B) : Standardization / Documents Updation
Sr. No. | Document Description | Put “#” on Applicable | Sr. No. | Document Description | Put “#” on Applicable
1. | Quality Alert |  | 8. | Work Instructions | 
2. | One Point Lesson (OPL) | # | 9. | Inspection Std. / Reports | 
3. | PFMEA / PQCS 2 |  | 10. | Packing Standard | 
4. | Control Plan |  | 11. | Process Flow Chart / PQCS 1 | 
5. | Poka Yoke Verification checklist |  | 12. | Drawings | 
6. | JH Checklist |  | 13. | Gauge / Jig / Fixture Drawings | 
7. | PM Checklist |  | 14. | Fixture Calibration Plan | 
Please Specify (if other, excluding above listed documents) |  |  |  |  | 
Sr. No. | Document Description | Put “#” on Applicable | Sr. No. | Document Description | Put “#” on Applicable
1. | Update in design. | # | 3. |  | 
2. |  |  | 4. |  | 
Note: Please put “ # ” mark for applicable / changed documents

## Slide 14
Thank you