## Slide 1: MAP ALLOYS
Analysis report and Action plan for Blow hole issue in Caliper Body-raw-REAR REML J1C.

## Slide 2
Process Flow Information
  Receipt of raw material
Incoming inspection of
AC2A Alloy
Incoming raw material inspection(Sand)
Storage of raw material.
Fettling/Grinding
Runner/Riser Cutting
Decoring
Casting
Note: Fill Red Color in process Block where defect is occurred.
Degassing (if DI not ok)
Holding molten metal in holding chamber
Melt treatment inside chamber and at holding chamber
Continuous charging and melting
DI and Spectro Check
N2 Lance Degassing
Die preparation & Die loading
Sand core
Heat Treatment
Heat Number punching & shot blasting.
Transfer to Inspection & Final inspection
Packing

## Slide 3
Root Cause Analysis: Ishikawa Diagram
Leakage issue Caliper body Raw-Rear REML-J1C.
Man
Machine
Method
Material
Measurement
Environment
Unskilled Operator
Machine Jerk and Vibration
Chemical composition not ok
Spectro not Calibrated.
Low illumination level (Rec: 600 min lux)
Pouring delay
Short pouring
Less metal temp.
Less die coat application
Machine parameters are not ok
Excess metal filling time.
New Operator
Wrong Grade material use.
Inspection frequency not defined.
Less venting
No smooth Feeding of metal in cavity.

## Slide 4
Validation of Probable Causes:
Sr. No. | Area/Condition | Probable Cause | Validation | Observation (Significant/ Non-Significant)
1 | Man | Unskilled Operator | Operator is skilled . | Non-Significant
 | Man | New Operator | Operator working from last 1.6 years | Non-Significant
2 | Machine | Machine jerk and vibration | No jerk and vibration in machine | Non-Significant
 |  | Machine parameters are not ok | Machine parameters like solidification | Non-Significant
 |  | Less Venting | Less gas pass from the cavity. | Non-Significant
3 | Method | Pouring delay by operator | No Pouring delay by Operator | Non-Significant
 |  | Short poring | No short pouring | Non-Significant
 |  | Less metal temp | Metal temperature found 718C | Non-Significant
 |  | Less die coat application | Die coat application found Ok | Non-Significant
 |  | Excess metal filling time | No excess metal filling time . | Non - Significant
 |  | No smooth Feeding of metal in cavity at leak area. | No smooth flow of metal due to pouring cup depth excess . | Significant
4 | Material | Chemical composition not ok. | Chemical composition found Ok | Non-Significant
5 | Measurement | Spectro machine not calibrated | Spectro machine calibrated. | Non-Significant
6 | Environment | Low illumination level (Rec: 600 min lux) | Lux level checked found - 760 | Non-Significant

## Slide 5
Why-Why Analysis for Occurrence:
Cause(s)  | Cause1 | Cause 2 (As Applicable)
Why- Why | Leakage after machining | 
Why 1 | Metal turbulence in cavity at blow hole area | 
Why 2 | No smooth flow of molten metal in cavity. | 
Why 3 | Pouring cup depth excess than required. | 
Why 4 |  | 
Why 5 |  | 
Final Root Cause | Pouring cup depth excess than required. | 

## Slide 6
Why-Why Analysis for Outflow :
Cause(s)  | Cause1 | Cause 2 (As Applicable)
Why- Why | Blow hole observed after machining | 
Why 1 | Internal defects open after machining. | 
Why 2 | Machining facility not available at our end. | 
Why 3 |  | 
Why 4 |  | 
Why 5 |  | 
Final Root Cause | Machining facility not available at our end. | 

## Slide 7
Verification of Corrective Actions
Sr. No. | Action taken | Verified By | Verification Date | Status | Remarks
1. | Pouring cup depth decrease and slop provided for smooth flow of metal in cavity. | Rajesh Pandey | 25.10.2024. | Completed | 
Note: Please attach evidences here. Insert evidences as objects.
Pouring cup depth decreases from 45mm to 32 mm for smooth pouring.
After Correction
Before Correction
Before correction pouring cup depth was 45 mm
After correction pouring cup depth was 32 mm

## Slide 8
Preventive Actions
Sr. No. | Action taken | Resp. | Target Date | Status | Remarks
1. | we will update in design of pouring cup. | Mr. Rajesh Pandey | 15.11.2024 | Completed. | 
Horizontal Deployment : |  |  |  |  | 
Sr. No. | Product Scope | Resp. | Impletn. Date | Status | Remark

## Slide 9
Thank you