## Slide 1
Supplier Name:- ANANT ENTERPRISES
Part category:- Bottom case
Monthly rejection analysis and Actions on vendor rating, Customer rejection / returns

## Slide 2
Part Name:- K0LA Drum
Defect:- Blow hole
Action plan for common defect on following parts

## Slide 3
Defect phenomenon in K0LA DRUM

## Slide 4
Sr. No. | 4M | Probable causes | Fact verification | Test Result | Remark
1 | Man | Operator skill | Skilled operator. | Found ok | Ok
2 |  | Operator process Knowledge | Operator have knowledge of process | Found ok | Ok
1 | Machine | Casting solidification timer | Solidification time 100+10 second | 100 sec | Ok
2 |  | Die temp veriation | Die temp found within specification. | 359°C | Ok
3 |  | Ejection not proper | Casting ejection done smoothly | Found OK | Ok
4 |  | Shrinkage feeding not proper | Blow hole open after buffing on ingate near oil seal OD. | Metal turbulence | Not OK
1 | Method | Die cleaning process | Die cleaning done as per decided frequency | Found ok | Ok
2 |  | Die maintenance | PM done as per the PM check sheet. | Found ok | Ok
3 |  | Die coating | Die coating done properly | Found OK | Ok
4 |  | Air vents cleaning | Air vents found OK | Found OK | Ok
1 | Material | Molten metal temperature. | Molten metal temperature found OK | 729°~743°C | Ok
2 |  | Inclusion / foreign particles in molten metal | Degassing done as per decided frequency | Found ok | Ok
3 |  | Degassing not done effectively | DI observed less than 2 | DI 0.4 Found ok | Ok
STUDY OF CAUSE & SIMULATION TEST

## Slide 5
Root cause analysis, Validation
Why:- Shrinkage feeding not proper near oil seal area
Why:- Turbulence create during molten metal pouring
Why:- Ingate thickness more than requirement of casting section
Root cause Validation
Part:- K0LA DRUM
Defect:- Blow hole
Ingate thickness more than requirement of casting section hence turbulence creates during molten metal pouring.
Turbulence resulted in to blow hole on ingate.

## Slide 6
THANKS