## Slide 1
ACTION PLAN
Customer Observation:- Sharp Edge at the End Coil ID.
DATE-12.08.2022
Customer Name :- ENDURANCE TECHNOLOGIES LTD.
SUPPLIER NAME :- HELICAL SPRINGS PVT. LTD.
PART NAME :- Rebound Spring (K0PG) PART No. :- (S2KH01502O)
Date :- 12/08/2022
NG
Sharp Edge (Burr) at the end coil ID

## Slide 2
Reoccurrence Prevention Why-Why Analysis [Outflow]
< WHY >
Outflow
Direct Cause
(1st)
Who
Inspector
3rd Cause
<Why>
Constitutional cause
<Management Issue>
Operator not check the mendral on time.
During Coiling stage mendral blunt.
Some of parts was made of Sharp edge.
Sharp edge at the End Coil ID. Not detected at final stage.
< WHY >
This problem have comes very rarely. Inspector was not aware about this issue.
Inspection of similar parts inadequate.
<Direct Cause>
< WHY >
2nd Cause
<Why>
Mendral frequency to cut spring is after 50,000.
(But the mendral was blunt before as it’s frequency decided.)
Sharp edge at the End Coil ID.
DATE-12.08.2022

## Slide 3
Corrective Action
Part Name – Rebound Spring K0PG
Part No-S2KH015020
DATE-12.8.2022
Mendral polishing frequency updated in tool monitoring sheet after 40,000pcs.
Training provided to operators.
BEFORE
AFTER
1.(a)
1.(b)
2.

## Slide 4
Preventive Action
Part Name – Rebound Spring K0PG
Part No-S2KH015020
DATE-16.8.2022
100% visual inspection at final stage.
Training provided to inspectors.
Quality Alert at final inspection stage.
Contentment Action:- Recheck 100% inspection of all WIP, In House & FG ‘ stock material.

## Slide 5
OPL
Part Name – Rebound Spring K0PG
Part No-S2KH015020
DATE-16.8.2022
NG
OK
ऊपर दिखाये गए चित्र K55G पार्ट मे ID BURR (Sharp Edge) है, जिस कारण से यह पार्ट NOT OK है।
ऊपर दिखाये गए चित्र K55G पार्ट मे ID मे कोई ID Burr नहीं है, इसलिए पार्ट ओके है।

## Slide 6
Updated the Final inspection std.

## Slide 7
Check Point added at Final Inspection

## Slide 8
Check point added at coiling
Before
After

## Slide 9
Thank You