## Slide 1
TUBE PRODUCTS OF INDIA
SHIRWAL
24th Feb- 2023
30x28-Saptagiri Engineering-Crack sample analysis.
Complaint 10/02/23

## Slide 2: Customer :- Saptagiri Engineering. Complaint :- Weld Crack. Size :- 30x28.

## Slide 3
Suspected lot details
Dispatches from Shirwal to PWH & from PWH to Saptagiri Engineering
Customer Name | PWH Invoice No. | PWH Invoice Date | OD | ID | Length | Qty Nos | Qty Mtrs | Qty Tons | Plant Invoice No. | Vehicle No. | Plant Invoice Date | LotQty
SAPTAGIRI | 3015010053327 | 27-Jan-23 | 30 | 28 | 4650 | 508 | 2540.4 | 1.78336 | PSH-LST-16302 | MH12MV1629 | 22-Dec-22 | 2651.8
SAPTAGIRI | 3015010053327 | 27-Jan-23 | 30 | 28 | 4650 | 22 | 111.4 | 0.0782 | PSH-LST-16302 | MH12MV1629 | 22-Dec-22 | 2651.8
SAPTAGIRI | 3015010053189 | 22-Jan-23 | 30 | 28 | 4650 | 343 | 1716 | 1.20463 | PSH-LST-16294 | MH12HD6776 | 20-Dec-22 | 8457
SAPTAGIRI | 3015010053189 | 22-Jan-23 | 30 | 28 | 4650 | 1348 | 6741 | 4.73218 | PSH-LST-16294 | MH12HD6776 | 20-Dec-22 | 8457

## Slide 4
Sr. No | Parameter | Specification (mm) | Actual (mm)
1 | OD | 30± 0.10 | 30.00/30.02
2 | ID | 28.0+0.075 | 28.04/28.08
3 | Crack length |  | 26.20
4 | Total length |  | 195
5 | Batch code |  | 02.02.23
Total Length-195 mm
Crack Area
Crack length- 26.20 mm
Sample photos & dimensions

## Slide 5
Failed Sample Analysis
Observation:-
Crack observed on the weld line.
Weak weld bond at defective area.
A
B
C

## Slide 6
Chemical Analysis
Chemical Composition |  |  |  |  |  |  | 
%Element | C | Mn | Si | S | P | Al | Remarks
Spec | 0.12 Max | 0.60 Max | - | 0.04Max | 0.04Max | - | 
Actual | 0.0975 | 0.3613 | 0.0059 | 0.0135 | 0.0175 | 0.0563 | OK
Remark:- Chemical Analysis by spectro Method does Confirms to IS 3074/2005 CEW 1

## Slide 7
Process Flow
CDW Tube Process Flow
End
Slitting
Tube Rolling
Annealing
Push Pointing/Swaging
Wet Process
Drawing
Straightening
ECT
Packing
Inspection
Cutting
Dispatch
Start
Weld Crack defect occurs in this area

## Slide 8
Wrong Tool used
Slit edge damage
Strip buckling due to speed mismatch in accumulator
Man
Method
Material
Machine
Weld Crack
Tooling
Un Skilled operator
Fin blade broken
Bearing failure
Impeder damage
Impeder Position not OK
Coolant contamination
Roll profile not okay
Mill alignment not ok
Slit edge burr
End weld strip off set
Speed and Power not as
per spec.
Root Cause Analysis:-
Root cause Analysis
Jerk during Rolling
Slit coil Camber
Side pressure clamp loose
Fin blade diameter
Slit edge offset during end weld joining
Fin cutting head

## Slide 9
# | 4M | PROBABLE CAUSES | FACTS VERIFICATION | Remark
1 | MAN | Wrong Tool used | Verified the tool issue process no abnormality observed | OK
 |  | Un Skilled operator | Operators are skilled no new operators on Machine | OK
2 | TOOLING | Roll profile not okay | Checked roll profile found ok | OK
 |  | Fin cutting head. | Fin Cutting head checked and observed top roll mounting pin worn out and damage .( Tube mill stoppage was there) | Not ok
 |  | Impeder damage | Impeder condition was ok | OK
 |  | Fin blade broken | No abnormality observed in Fin blade | OK
 |  | Fin blade diameter | Fin blade diameter is inadequate when end weld is offset | ok
3 | MATERIAL | Slit edge damage | Wooden plank on slit storage rack found | OK
 |  | Slit edge burr | No burr observed on slit | OK
 |  | Slit coil thickness variation in initial lap | No Thickness variation in initial lap of slit coil | OK
Verification of Causes

## Slide 10
# | 4M | PROBABLE CAUSES | FACTS VERIFICATION | Remark
4 | METHOD | Mill alignment not ok | Mill alignment checked during setting found in place. | OK
 |  | Speed and power as per specification | Speed and power checked as per speck and found ok. | OK
 |  | Slit edge offset during end weld joining | Parallel Slit edges are verified by visually | OK
 |  | Impeder Position not OK | Fin cutting bar length is standardized and it is OK | OK
5 | MACHINE | Strip buckling due to speed mismatch in accumulator | Tube mill accumulator potentiometer found OK | OK
 |  | Bearing failure | No bearing failure found | OK
 |  | Coolant contamination | Filter checked found OK | OK
 |  | End weld strip off set | The operation of Strip joining was carried out by hydraulic system | OK
 |  | Side pressure clamp got loose. | No strip shifting observed. | OK
 |  | Jerk during Rolling | Verified the Tube mill report no Mill jerk observed | OK
Verification of Causes

## Slide 11
(WHY-WHY ANALYSIS)
WHY – 1 | WHY- 2 | WHY -3 | WHY-4 | Why-5
Weld Crack. | Weak weld bond | Improper squeezing during welding at localized area due to Fin cutting disturbance | Fin Cutting head top roll momentary blockage | Fin Cutting head top roll mounting pin worn out and damage
● Root cause establishment (Why-Why Analysis) - Occurrence
● Root cause establishment (Why-Why Analysis) - Detection
WHY – 1 | WHY- 2 | WHY -3 | WHY-4 | Why-5
Weld crack | Tube got opened in sub sequent operation | Less bonding strength | Not detected in ECT | Weld intact.

## Slide 12
Action Plan
Occurrence Side Action |  |  |  | 
Sr. No | Cause | Countermeasure | Target. Date | Status
1 | Improper squeezing during welding at localized area due to Fin cutting disturbance | 1.In every rolling of final30x28 size Fin cutting head top roll pin will be replaced with new pin. 2) Pin change point added in Fin cutting tool issue check sheet. | 1) 05/03/23 2) Added on 22/02/23 | 2) Completed
Detection side Action |  |  |  | 
1 | Detection | As per Stoppage Matrix one extra tube will be removed. | Implemented by Jan-23 | Started.
2 |  | On line ECT at TM 2 Planned. | May-2023 | 

## Slide 13: Thank You !