## Slide 1
Forming at one side , As installed new carbide bush into mounting bottom block , It has tapper up to 1.0 mm | Carbide bush verified for parallelism . Observed parallelism up to 1.0 mm its rework grinding operation. After rework Carbide bush verified and its observed 0.12 mm Made a SOP for carbide bush installation. At stored location, All carbide bush verified. While production , First part of the shift its’ verify by Profile projector. Awareness training provided to final inspector
ACTIONS FOR BOTTOM CAP OFFSET PUNCHING
Supplier: Saptagiri Industries.
Operation: Bottom cap Offset punching
Implementation Date: 18.04.2023
BEFORE
AFTER
Problem/Present Status: Bottom cap. Offset Punching
RM inspection
Sheet shearing
Blanking
Material flow
Forming
Forming at one side , As installed new carbide bush into mounting bottom block , It has tapper up to 1.0 mm
RM inspection
Forming
Material flow
Sheet shearing
Blanking
Packing
Final Inspection
Packing
Face Turning
Final Inspection
Face Turning
Made a SOP for carbide bush installation
While production , First part of the shift its’ verify by Profile projector.
After rework Carbide bush verified and its observed 0.12 mm
Observed parallelism up to 1.0 mm its rework grinding operation
Carbide bush verified for parallelism