## Slide 1
While blanking operation, sheets’ sharp edges draw Same scratches line mark will generate on parts | Sheet sharing operation eliminate Material will procure in coil form Sheet drawing while part producing avoided
ACTIONS FOR LINE MARK ( WASHER S2PL03812B)
Supplier: Saptagiri Industries.
Operation: Press shop / Machine shop
Implementation Date: 10.06.2023
BEFORE
AFTER
Problem/Present Status: Stamping mark like depth line mark at top surface of Washer K55G.
Material flow
While blanking operation, sheets’ sharp edges draw
Sheet drawing while part producing avoided
Same scratches line mark will generate on parts
Sheet sharing operation eliminate
Material will procure in coil form
Raw material Inward
Plating
Sheet Sharing
Bblanking & Center hole piercing
Final Inspection
Packaging
Material flow
Raw material Inward
Plating
Coil form
Bblanking & Center hole piercing
Final Inspection
Packaging