## Slide 1: Action plan Dt.:28 Jun 2023

## Slide 2
CONDITIONS FOR OCCURRENCE
● Phenomenon: Welding line open parts.
Trouble content
・Supplier: Endurance tech.
・Model: Kawasaki
・Parts name: Adjuster
・Part No.: S2AB04412O
・Date of Occurrence: 28.06.2023
・Qty NG: 2000 Nos.
●Parts Stock check results
Action
Area | Total Stock | Checked | Checking Method | NG Qty | Status
ETL – K120 | 2000 | 2000 | Visual check | 228 | All available stock qty. Rejected
NG Part | OK Part
Welding line Open
No weld line open

## Slide 3
UNDERSTANDING OF ACTUAL CONDITION AND CONTROL
Process Flow
Possible defect occurrence area.
Raw Material Inward
Sheet Shearing
U Bending
First Rounding
Second Rounding
CO2 Welding
(Single Spot)
Blanking
Co2 Welding
(Full Run)
Weld Bead Turning & Grinding
Buffing
Single Notch
Restracking
First Flaring
Parting & ID Chamfer
Buffing
Second Flaring
Face Deburring
Packing/storing
OD Trimming & 8 nos Notching
Final Inspection
Fe Zn Plating

## Slide 4
UNDERSTANDING OF ACTUAL CONDITION
● Understanding the actual cause – (Factor analysis)
Man
Method
Material
Machine
Welding Open after buffing operation
Less Awareness
Round Bending not uniform (Circular
Uneven Round Bending
Round Bending Gap uneven
Round Bending Gap More
Excess welding outside the Gap
Gap not filled by welding
Excess Buffing on welding area
Sample Basis Inspection
Uneven welding

## Slide 5
# | 3M | PROBABLE CAUSES | FACTS VERIFICATION | Jud.
1 | MAN | Less Awareness | Operator and inspector not aware about the weld line open | O
2 | MACHINE | Round Bending not uniform (Circular) | Round bending observe uniform ( Circular ) | O
 |  | Uneven round bending | Height variation in both side as well as uneven gap | 
 |  | Round bending gap uneven | In a few part observed uneven gap at top side less ( 0.54 mm ) and bottom side more (1.44 mm ) | 
 |  | Excess welding outside the gap | No Excess buffing observed | O
 |  | Gap not filled by welding | Gap fully filled by welding operation | O
 |  | Gap not filled by welding | Gap fully filled by welding operation | O
 |  | Excess buffing on welding bead area | No Excess buffing on welding line | O
 |  | Excess buffing on welding bead area | No Excess buffing on welding line | O
 |  | Uneven Welding | Welding run verified and observed evenly ( In straight line ) | O
4 | METHOD | Sample basis Inspection | While welding and buffing operation only do the sample basis inspection | 
FACTS VERIFICATION

## Slide 6
ROOT CAUSE ESTABLISHMENT (WHY-WHY ANALYSIS)
 | WHY – 1 | WHY- 2 | WHY -3 | WHY-4 | Why-5 | Why-6
Occurrence | Welding Open after buffing operation | Uneven round bending / Round bending gap uneven | Ram entry less or raw material spring back |  |  | 
Outflow | Welding Open after buffing operation | No Inspection after the buffing operation |  |  |  | 
Conclusion
Uneven round bending / Round bending gap uneven
Ram entry less or raw material spring back
No Inspection after the buffing operation
Inspection after the buffing operation
● Root cause establishment (Why-Why Analysis)

## Slide 7
COUNTERMEASURES
 | Cause | Countermeasure | Tgt. Dt. | Status
Supplier End | <Occurrence > | Before Welding operation 100% inspection starts for uneven round bend. 100% inspection starts after welding operation. Draw route process to be introduce instead of welding process. ( Sample Submitted for final approval ) | 30-06-2023 30-06-2023 30-06-2023 | Completed Completed Completed
Supplier / ETL End | <Outflow> | 200% Inspection started along with marking at inner side at Final Inspection. Q-Alert display at Final inspection and welding stage. Training given concern operator and inspector for uneven bending and welding open after the buffing process. | 30-06-2023 30-06-2023 30-06-2023 | Completed Completed Completed

## Slide 8
Welding process and draw route process :

## Slide 9
Q–Alert display at work places :

## Slide 10
Training record :
100% Inspection Identification mark
Awareness training for uneven gap for welding
Awareness training for weld line open after forming operation
200 % Inspection weld crack ( Weld line open )

## Slide 11: THANK YOU