## Slide 1
AFTER
BEFORE
DRILL MACHINE :- SE/CNC/05 Date: 18/04/022
Problem/Present Status:
Burr cleaning done thru air pressure , improper cleaning because there is no under cut in clamping chuck jaw, burr, chip not removed from Chuck jaw properly.
Countermeasure:
Benefits :- Excess parallelism defect phenomena eliminated.
Countermeasure:- Machining stage

## Slide 2
AFTER
BEFORE
DRILL MACHINE :- SE/CNC/05 Date: 18/04/022
Problem/Present Status:
Countermeasure:
Cleaning started thru air gun by providing high air pressure (4 Bar), burr chip removed from chuck jaw properly and defect eliminated because under cut added up to 1.5mm.
Benefits :- Excess parallelism defect phenomena eliminated.
Countermeasure:- Machining stage