## Slide 1
Fishbone
1
2
Occur / Outf. | Problem | Why-1 | Why-2 | Why-3 | Why-4
Occurrence | Flatness Obs. 0.30mm Against 0.20mm | Improper Lug Matching Sequence | Lug Matching Sequence was Found Disturbed | Due to improper material handling during heating | Possibilities was not Considered in Heating W.I
Outflow | Flatness Obs. 0.30mm Against 0.20mm | Improper Inspection | Defected Parts was Not Detected During Sampling Inspection | Sample Collected From one Box | Check Point was not Available for Sample Collected from Multiple Boxes.
Man
Machine
Sr. No. | Probable Cause | Verification | Jud (O/X)
1 | Negligency Done by Inspector | Training record available for same | O
2 | Heating parameter disturb | Heating Parameter Observed 261˚C against 270±20˚C | O
3 | Improper Lug Matching Sequence | Lug Matching Sequence was Disturb | x
4 | Un-even Holding Time | Holding Time Found ok (40 Minutes) | o
5 | Improper Inspection | Sample Collected from One Box | x
Probable Causes
3
Occurrence Countermeasure | Illustration
Check has been Added in Heating W.I . OPL Has been made for Lug Matching Sequence.. PFMEA Has been updated for lug Matching Training Provided to the Operator. | 
All actions horizontal development in all Core Plate | 
4
5
Outflow Countermeasure | Illustration
Final Inspection W.I has been Updated. Training to be given to the concerned persons. Sampling inspection has been started to collect the sample from multiple Boxes. 100% marking has been Implemented on Outside of the Bunch SOP made and adhere for flatness checking | 
Note : All countermeasure will be implemented-Done
6
Material
Method
Problem :-
Flatness Obs. 0.30mm Against & Nov’23 0.20mm in LML core Plate & 3W4S
Improper lug Matching Sequence
Negligency Done by Inspector
Improper Inspection
Un-Even Holding Time
Heating Parameter Disturb
OPL
Heating Work Instruction
Final Inspection W.I
Training

## Slide 2
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken (Cause Side)
Possibilities was not considered in Heating W.I
Check Point has been added in heating W.I
W.I
W.I

## Slide 3
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken -Cause Side
Possibilities was not considered in PFMEA
Lug matching issue covered in PFMEA and adhered

## Slide 4
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken -Cause Side
Lug Matching was Disturbed During Heating Process
#Training provided for Proper Lug matching Sequence to Avoid Flatness Issues
#OPL made and adhere

## Slide 5
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken -Cause Side
Check Point not Covered in Final Inspection W.I
Check Point Covered in Final Inspection W.I.
Training provided

## Slide 6
Actions Taken- Before/After
NA
BEFORE
AFTER
Problem
Improvement
Actions Taken -Cause Side
OPL has been Made and Displayed at Concern Department

## Slide 7
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken -Cause Side
Tie bar bolt locking mechanism was not available
Tie bar bolt locking mechanism has been Made and adhered.

## Slide 8
Actions Taken- Before/After
NA
BEFORE
AFTER
Problem
Improvement
Actions Taken -Cause Side
SOP made and adhere for flatness inspection & Gauging

## Slide 9
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken (Inspection Side)
Marking was not available on parts
100% marking has been Implemented on Outside of the Core Plate Bunch

## Slide 10
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken (Inspection Side)
Q-Sustenance Monitoring Sheet Has been Started
N/A

## Slide 11
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken -Inspection Side
Receiving Gauge Validation Plan was not adhered
# Gauge verification started on daily basis from 6 months
# SOP made for inspection and verification –Done
# Training Provided

## Slide 12
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken (Cause Side)
Possibilities was not considered in Machine Check Sheet
Check Point has been added in Daily PM Check sheet
Daily PM Check Sheet
Daily PM Check Sheet

## Slide 13
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken (Inspection Side)
OPL made for inspection by snap gauge & training given for the same.
N/A

## Slide 14
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken (Inspection Side)
Q-Sustenance Monitoring Sheet Has been Started and adhered.
N/A