## Slide 1
Fishbone
1
2
Occur / Outf. | Problem | Why-1 | Why-2 | Why-3 | Why-4
Occurrence | Flatness Obs. 0.30mm Against 0.20mm | Improper Lug Matching Sequence | Lug Matching Sequence was Found Disturbed | Due to improper material handling during heating | Possibilities was not Considered in Heating W.I
Outflow | Flatness Obs. 0.30mm Against 0.20mm | Improper Inspection | Defected Parts was Not Detected During Sampling Inspection | Sample Collected From one Box | Check Point was not Available for Sample Collected from Multiple Boxes.
Man
Machine
Sr. No. | Probable Cause | Verification | Jud (O/X)
1 | Negligency Done by Inspector | Training record available for same | O
2 | Heating parameter disturb | Heating Parameter Observed 261˚C against 270±20˚C | O
3 | Improper Lug Matching Sequence | Lug Matching Sequence was Disturb | x
4 | Un-even Holding Time | Holding Time Found ok (40 Minutes) | o
5 | Improper Inspection | Sample Collected from One Box | x
Probable Causes
3
Occurrence Countermeasure | Illustration
Check has been Added in Heating W.I . OPL Has been made for Lug Matching Sequence.. PFMEA Has been updated for lug Matching Training Provided to the Operator. | 
All actions horizontal development in all Core Plate | 
4
5
Outflow Countermeasure | Illustration
Final Inspection W.I has been Updated. Training to be given to the concerned persons. Sampling inspection has been started to collect the sample from multiple Boxes. 100% marking has been Implemented on Outside of the Bunch SOP made and adhere for flatness checking | 
Note : All countermeasure will be implemented-Done
6
Material
Method
Problem :-
Flatness Obs. 0.30mm Against & Nov’23 0.10mm in core Plate 3W4S
Improper lug Matching Sequence
Negligency Done by Inspector
Improper Inspection
Un-Even Holding Time
Heating Parameter Disturb
OPL
Heating Work Instruction
Final Inspection W.I
Training

## Slide 2
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken (Cause Side)
Possibilities was not considered in Heating W.I
Check Point has been added in heating W.I
W.I
W.I

## Slide 3
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken -Cause Side
Possibilities was not considered in PFMEA
Lug matching issue covered in PFMEA and adhered

## Slide 4
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken -Cause Side
Lug Matching was Disturbed During Heating Process
#Training provided for Proper Lug matching Sequence to Avoid Flatness Issues
#OPL made and adhere

## Slide 5
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken -Cause Side
Check Point not Covered in Final Inspection W.I
Check Point Covered in Final Inspection W.I.
Training provided

## Slide 6
Actions Taken- Before/After
NA
BEFORE
AFTER
Problem
Improvement
Actions Taken -Cause Side
OPL has been Made and Displayed at Concern Department

## Slide 7
Actions Taken- Before/After
NA
BEFORE
AFTER
Problem
Improvement
Actions Taken -Cause Side
SOP made and adhere for flatness inspection & Gauging

## Slide 8
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken (Inspection Side)
Marking was not available on parts
100% marking has been Implemented on Outside of the Core Plate Bunch

## Slide 9
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken -Inspection Side
Receiving Gauge Validation Plan was not adhered
# Gauge verification started on daily basis from 6 months
# SOP made for inspection and verification –Done
# Training Provided

## Slide 10
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken (Inspection Side)
OPL made for inspection by snap gauge & training given for the same.
N/A

## Slide 11
Actions Taken- Before/After
BEFORE
AFTER
Problem
Improvement
Actions Taken (Inspection Side)
Q-Sustenance Monitoring Sheet Has been Started and adhered.
N/A