## Slide 1
Action Plan Customer Complaint
Part Name | Defect Phenomena | Rejection Qty | Defect Photograph | Root Cause (Why-Why Analysis) | Counter Measure (Action Plan) | Target Date | Evidence | Status
DX 101004 (Gear Primary Driven K70) | OPD Over size Observed o.12 MM (115.792-0.072 to -0.222 mm) | 1 |  | Occurrence (Cause) Side:- Why1:-Without teeth sheaving components dispatch to ETL Why2-For sheaving components and without sheaving component store same location on machine Why3-Mixup Possibility not identified Why4-Sheaving operation ok components storage location not identified on machine | Occurrence (Cause) Side:- 1)Different arrangement provided for storage of with sheaving and without sheaving material. 2) Hanger attached to sheaving machine for storage sheaving output components. | 22.08.2023 5.08.2023 |  | 
 |  |  |  | Outflow (Inspection/System) Side:- OPD inspection done on manual dial type OPD fixture Part DFCE inspection done on manual rolling tester | Digital Display type gauge will be provided for OPD inspection at final inspection stage . Auto roll tester provided for DFCE Inspection. | 28.8.23 22.8.23 |  | 
With Sheaving
For Sheaving