## Slide 1
MAP ALLOYS

## Slide 2
Sr No | Part Name /No | Defect /Qty Rej | Why Why Analysis | Action Plan | Resp | Target Date | HD | Status
2. | -HOLDER BRACKET BODY RAW CASTING C101 /B2FP02303O | Blow hole – 280 Nos | Why 1- After machining blow hole observed at customer end . Why 2: Air interrupted at the time of Metal pouring. Why 3: Slits not provided to escape from die cavity. | Action Plan: 1.Slits provided in die t | 1.Mr. Dhande. | 1.10.03.2024 | Applicable for All Master cylinder Family | 1.Completed
Blow hole action plan for B2FP02303O-HOLDER BRACKET BODY RAW CASTING C101

## Slide 3
Before
After
Air slits provided in Die to escape air from cavity of die .
No
No slits provision in this Die to escape air from cavity of die .
Blow hole action plan for B2FP05303O-HOLDER BRACKET CASTING -REML REAR J1C

## Slide 4
THANK YOU