## Slide 2: BEFORE-AFTER DATE – 19.06.2024
AFTER
BEFORE
Silver paint( Craftnol 104 M ) applied at sand core profile area.
No paint applied at sand core profile area
TVS N TORQUE CALIPER– OBSERVED SAND DROP ISSUE .
PREPARED BY- PATIL K L APPROVED BY – D B LAD